Fluorinated Ladder Polymer Membranes for Targeted Separation of High Global Warming Potential (GWP) Refrigerants

Benjamin Kamji and Ruilan Guo*

Department of Chemical & Biomolecular Engineering, University of Notre Dame, Indiana, 46556, United States

* Corresponding author: rguo@nd.edu

ABSTRACT

The separation and recovery of hydrofluorocarbon (HFC) refrigerant blends is an emerging technological challenge driven by regulatory mandates targeting the phase-down of high global warming potential (GWP) gases. Conventional polymer membranes have low flux and suffer from severe plasticization under highly condensable fluorocarbon exposure, leading to selectivity loss at elevated pressures. Here, we report a new class of fluorinated ladder polymers of intrinsic microporosity (PIM-F) by incorporating decafluorobiphenyl (DFBP) moieties to engineer sorption-driven selectivity and suppress pressure-induced plasticization. By systematically varying DFBP incorporation, we tune free volume distribution, fluorophilic interactions, and chain rigidity. Dense and free-standing defect-free films demonstrate exceptional R-32/R-125 selectivity of about 51 and 62 for the 50% and 75 % copolymer compositions with very high permeabilities under operating pressures up to 100 psi. Structure–property correlations reveal that increasing fluorination enhances plasticization resistance while preserving favorable permeability–selectivity tradeoffs. This membrane platform provides a scalable, energy-efficient pathway for refrigerant separation and reclamation and supports environmentally compliant HFC recovery.

KEYWORDS: HFC, GWP, Plasticization, fluorophobic, moieties, intrinsic, microporosity, free volume, selectivity, permeability reclamation,

- INTRODUCTION

Hydrofluorocarbons (HFCs) have long served as working fluids in vapor-compression refrigeration systems due to their desirable chemical stability and thermodynamic properties. However, many HFCs exhibit extremely high global warming potentials (GWPs), prompting phasedown under international regulatory agreements such as the Kigali Amendment and U.S. AIM Act. The demand for high-performance refrigeration and air conditioning (RAC) is projected to rise sharply as global temperatures increase and populations grow in hot, densely populated regions, driving sustained growth in cooling energy use and refrigerant consumption.1,2 Due to surging demand, the global stock of air conditioners is projected to grow from about 1.6 billion units to 5.6 billion by 2050, equivalent to roughly five units sold every second over the next few years3–5.

Current vapor-compression systems rely heavily on the blends of these fluorinated gases (primarily hydrofluorocarbons (HFCs) with some hydrofluoroolefins (HFOs) that are designed to balance thermodynamic efficiency, flammability, and toxicity. Yet, many widely deployed HFC-rich mixtures still exhibit very high global warming potentials thousands of times higher than CO₂ and have long atmospheric lifetimes which remain major contributors to global warming.6–9 In efforts to curb further climate warming, fluorinated greenhouse gases known as F-gases especially hydrofluorocarbons (HFCs) used in HVAC (Heating ventilation and air-conditioning) systems represent one of the most critical challenges as their contribution to total greenhouse gas emissions is projected to rise rapidly if unchecked. However, the Kigali Amendment to the Montreal Protocol enforced in 2019, establishes a global commitment to limit HFC production and use to avoid up to half a degree of additional warming by 2100. 5,17 To meet these goals, there is a demand to phase down high-GWP refrigerants in many applications by imposing steadily shrinking quotas on the production and import of HFCs, and tightening requirements for leak prevention, recovery, recycling, and destruction at equipment end-of-life to minimize fugitive emissions. This stringent policy landscape is forcing the refrigeration market to seek innovative technical solutions, as widely used blends such as R-410A (GWP =2088) which is an equimass mixture of difluoromethane (R32, GWP=675) and pentafluroethane (R-125, GWP=3500), needs to be separated. This value-added R32 needs to be preferentially separated from the refrigerant blend R410A for the final goal of reblending with other HFOs for the reformulation of new HFC/HFO low GWP refrigerant mixtures.18

Nevertheless, several strategies have been considered for the separation of HFCs and other refrigerants. Shiflett and Yokozeki19,20 proposed deploying ionic liquids (ILs) as entrainers in extractive distillation towers to effectively separate R32 and R125 from the R410A blend. Selective adsorption using porous materials such as zeolites, metal-organic frameworks (MOFs), Covalent-organic frameworks (COFs) and activated carbons was considered as another suitable alternative for the preferential uptake of one of the components over others in the HFC blend. 6,8,10  While these advanced separation technologies are commendable, their substantial energy demands underscore the need for more energy-efficient separation alternatives. Membranes offer a promising and unique opportunity for separating high-GWP mixtures, providing key advantages such as low energy requirements, reduced operating costs and spatial requirements, small footprints and the ability to leverage differences in chemical structure to drive permeability and selectivity. 21,33–34 To the best of our knowledge, the separation of refrigerant molecules remains largely under-investigated, with only a handful of studies reported in the literature. Pardo et al. reported the separation of HFC-32(dichloromethane), HFC-134a (1,1,1,2-tetrafluoroethane, CH2FCF3) and HFO-1234yf (2,3, 3,3-tetrafluoropropene) using varying compositions of poly(ether-block-amide) (PEBAX) membranes. 37,39

On the other hand, glassy polymers with high fractional free volumes such as PIMs (polymers of intrinsic microporosity) have emerged as leading membrane materials for gas separations over the past two decades. Budd et al. first characterized PIM-1's rigid, contorted spiro-center structure, which limits chain rotation and packing to deliver exceptional microporosity and free volume beyond conventional glassy polymers32,34,44 Gutierrez-Hernandez et al. further reported that polymers of intrinsic microporosity are well-suited for this kind of separation due to their size-sieving ability.34,36,41.

Despite their exceptional separation performance, PIM-1 membranes suffer from plasticization, which refers to the swelling of the polymer matrix under high partial pressures of condensable penetrants or diluents, allowing more segmental chain motion and leading to an overall decline in selectivity. In this regard, great efforts have been made to reduce such effects by techniques such as the creation of mixed matrix membranes (MMMs) via the incorporation of inorganic fillers to PIM-1 matrix and via chemical crosslinking or rigidification. Strategies to suppress plasticization in high–free-volume glassy polymers largely parallel those developed to address physical aging, but the underlying mechanistic targets differ. In MMMs, the addition of non-collapsible, dimensionally stable fillers serves to mechanically anchor the polymer matrix and suppress the dilation that accompanies penetrant sorption. These fillers reduce the extent of polymer chain relaxation by imposing geometric confinement and lowering the effective swelling of the membrane. Chemical crosslinking represents a more direct method of suppressing plasticization by forming chemically bonded linkages or connections that will restrict segmental motions and large-scale rearrangements of polymer chains from condensable penetrants. This is typically achieved by incorporating functional groups along the polymer backbone or chain ends, which can help reduce the dilation effects from these condensable gases.  Halogenated systems, particularly fluorinated moieties, are known to suppress such effects and positively influence gas transport in glassy membranes; however, the magnitude of these effects remains poorly understood and quantified.

In this work, we hypothesize that incorporating bulky fluorinated moieties into the PIM-1 backbone will increase the sorption selectivity for the more condensable HFC gas and raise or maintain permeability via fluorine-induced free-volume expansion, enabling preferential uptake of one HFC penetrant over another. This study seeks to rigorously probe this hypothesis by systematically varying the degree of backbone fluorination in PIM-1 and quantifying the resulting changes in gas transport properties. Typically, the only tunable structural parameter is the degree of fluorination, which is empirically controlled by reaction time. To accomplish this, fluorinated random copolymers of intrinsic microporosity known as PIM-Fx were created by incorporating    Decafluorobiphenyl (DFBP) as the fluorinated comonomer to modulate chain packing, intersegmental interactions and gas-polymer affinity. These polymers were designed and synthesized to study the effect of fluorination on the gas permeation properties of R410A to establish a detailed composition -dependent structure-property relationship that demonstrates unprecedented membrane performance for HFC separation.

- EXPERIMENTAL

2.1 Materials

Tetrafluoroterephthalonitrile 99% (TFTPN) and decafluorobiphenyl 99% (DFBP) were purchased from Sigma-Aldrich and used as received. 5,5′,6,6′ Tetrahydroxy-3,3,3′,3′-tetramethyl-1,1′-spirobisindane (TTSBI, 97%) was purchased from Thermo Scientific and used as received. Potassium carbonate and anhydrous dimethylformamide (DMF) were purchased from Sigma-Aldrich and used as received. Chloroform and methanol were both purchased from VWR and were used as received.

2.2 Synthesis of PIM-1

High-molecular-weight PIM-1 was synthesized using the conventional low-temperature method to benchmark PIM-Fx copolymers synthesized at high temperature. Specifically, TTSBI was mixed with TFTPN and potassium carbonate at a 1:1:2.05 molar ratio in DMF placed in a 100ml three-necked round-bottom flask equipped with a reflux condenser and a magnetic stirring bar. The mixture was stirred at 60 °C under a positive nitrogen atmosphere for 72h. After three days, the solution was precipitated into a 1:1 (v/v) mixture of methanol and water and then filtered. The crude yellow product was dried at 100 °C overnight in a standard laboratory vacuum oven. The filtrate was re-dissolved in chloroform and reprecipitated into pure methanol and then dried in the vacuum oven again under the same conditions. This step was carried out at least once to purify the polymer and to wash away any low molecular weight chains.

2.3. Synthesis of PIM-Fx Copolymers

Fluorinated ladder polymers of intrinsic microporosity (PIM-Fx) were synthesized via nucleophilic aromatic substitution (SNAr) polycondensation reaction between TTSBI, TFTPN, and the fluorinated comonomer, DFBP (decafluorobiphenyl). The fluorinated copolymers exhibiting varied degrees of fluorination are shown in Scheme 1. This variation was done by adjusting the molar ratio between TFTPN and DFBP to generate a copolymer series denoted as PIM-Fx, where x represents the mol% of DFBP. A typical copolymer synthesis is as follows using PIM-F0.5 copolymer as an example: TTSBI (1.5g, 4.4mmol) was mixed with potassium carbonate at a 1:2.05 molar ratio in 10 ml DMF, placed in a 100 ml dried three-necked round-bottom flask equipped with a reflux condenser and a magnetic stir bar. The mixture was stirred at 100 °C under a positive nitrogen atmosphere for 30 mins. Simultaneously, TFTPN (0.43 g, 2.15mmol) and DFBP (0.72 g, 2.15mmol) were dissolved in 36.5 mL anhydrous DMF based on a 5.7 wt%/v reaction concentration at room temperature and transferred into the reaction mixture drop-wisely using an addition funnel. The reaction was maintained at 100 °C for 2 h (50% and 75% DFBP mol%) and 3 h (10% and 25% DFBP DFBP mol%) for different fluorination levels until a yellow suspension was obtained with close monitoring checks to ensure that gelation and possible branching were avoided due to DFBP's high reactivity. However, the reaction for the homopolymer was left for 48 h following already established procedure by Fuoco et al.46 These suspensions were quenched into 150 mL of aqueous methanol and HCl (5 v/v%), and the precipitate was filtered by a sinter funnel under vacuum. The crude yellow product was dried at 100 °C overnight in the vacuum oven. The polymer product was then re-dissolved at least once in chloroform and reprecipitated into pure methanol and then dried in the vacuum oven again under the same conditions. This step was necessary to effectively purify the polymer and to wash away any low molecular weight chains.

Scheme 1. Synthesis of fluorinated PIM copolymers (PIM-Fx) exhibiting systematically varied degrees of fluorination

2.4. Film casting and stabilization

Thin films of pure PIM-1 and PIM-F copolymers were prepared via a solution casting method. In a typical case, polymer was prepared in a 3% w/v solution in chloroform and filtered through a 1μm Teflon syringe filter and cast in a covered Petri glass dish for 3-4 days at room temperature. The films, which self-detached from the glass surface of the dish over this period, were then soaked for 24 hours in methanol, then dried in a vacuum oven at 100 °C for one hour to remove residual solvent prior to gas permeation testing. Each film’s thickness was confirmed to be between 80-120 µm with a micrometer gauge.  The freshly prepared films were then immediately used for gas permeation testing, structural characterization, and other detailed analysis. Representative pictures of the prepared thin films are in Figure 1.

Figure 1. Optical images of free-standing, solution-cast PIM-1 and PIM-F films

2.5. Characterization Methods

1H and 19F nuclear magnetic resonance (NMR) spectroscopy were conducted on a Bruker AVANCE III HD 400 Nanobay spectrometer using CDCl3 as a solvent. Fourier-transform infrared spectrometry (FTIR) was performed on a JASCOFT_IR6300 spectrometer at a 4cm-1 resolution with 64 scans. Thermogravimetric Analysis was performed using TGA Q2500 instrument under 30ml/min of N2. Wide-angle X-ray scattering (WAXS) was performed using a MalvernAeris benchtop XRD set to reflection mode at 40mA and 40KV using a Cu Kα radiation source with a wavelength of 1.54Å. The d-spacing was calculated using Bragg’s law, where the detector’s radiation wavelength is divided by two times the sine of the beam angle. GPC was performed using linear PS (polystyrene) polymer as standard with THF as the eluent at at 35 °C with THF flow rate = 1.0 mL/min, a differential refractive index (RI) detector (Wyatt Technology, Optilab T-tEX) using PSS WinGPC 7.5 software.  The density of the polymer films was determined via the buoyancy method in room temperature dionized water (water uptake in the hydrophobic , glassy polymer films was negligible) using a Mettler ToledModel ML204 density Kit coupled to an analytical balance. Using f=data provided by the density measurements, fractional free volume (FFV) of the films were calculated via the Bondi group contribution method.

2.6. Gas Permeation Measurements and Plasticization Studies Experiments

Pure gas permeabilities, P, in Barrer (1Barrer = 10 -10  cm3 (STP) cm/cm2 s cm Hg), of R-32, R-125, were measured in a fixed volume variable pressure gas cell. The heater was set to 35 °C using a water bath to control the temperature, while the downstream was pulled to a vacuum by a Welch DuoSeal vacuum pump and had pressure monitored by a MKS Barotron transducer with a range up to 11 torr. Experimentally, several film samples of each composition were prepared and tested, and permeation data averaged from multiple measurements were reported to ensure reliable comparisons. Typical procedure would have the permeation samples loaded into the cell and tested under 30psi of nitrogen to check for pinholes before they were degassed for at least 12 h under vacuum. Both the upstream and downstream were then sealed off and the pressure was measured for an hour to obtain the leak rate of the downstream, after which the films were tested at 35 °C at 30, 50, 80, and 100 psi for R-32 and R-125. The steady state permeabilities of the films were determined using equation 1:

P= 1010Vd lpupRTA dpdtss-dpdtleak

where Vd is the downstream pressure in cm3, l is the thickness of the film sample in cm, pupis the upstream pressure in cmHg, A is the area of the membrane sample in cm2, R is the gas constant (0.278 cm3 cm Hg/cm3(STP)*K), T is the temperature in K, (dp/dt)ss and (dp/dt)leak in cmHg/s are the pressure change rate in the downstream and the leak rate, respectively. The selectivity of gases, αx/y, is then defined as the ratio of permeabilities of the gas, with the more permeable gas being the numerator αx/y=Px/Py.  To study fundamental gas transport properties, sorption measurements were performed as the time-lag method would be quite inaccurate to estimate the diffusivity based on the nature of the gas molecules and also due to the fast-permeating nature of PIM-1t.  The diffusivity of our gas pairs could be determined using the solution-diffusion model in equation 2 :

P = D × S

- RESULTS AND DISCUSSION

3.1. PIM-Fx Synthesis and Characterization

A series of high molecular weight fluorinated PIM-Fx copolymers was synthesized to map detailed structure–property relationships governing the transport of condensable HFC gases. These copolymers were synthesized by adjusting the feed molar ratio between the comonomers DFBP and TFTPN, which were copolymerized with TTSBI to enable thorough investigation of fundamental structure-property relationships. Following the successful synthesis of the copolymer series, chemical structures were validated using 19F NMR and 1H spectroscopy as seen in Figure 2. Specifically, the marked peaks 1, 2, and 3 at -138 ppm, -141 ppm and -162 ppm correspond to DFBP moieties in the 19F NMR spectrum in Figure 2A. As seen in Figure 2B, the  1H resonances at approximately 1.3 ppm (a), 2.2 ppm (b), 6.7 ppm (c), and 6.3 ppm (d) are attributed to the TTSBI moieties. With increasing fluorination, peak d shifts progressively downfield (to the left), reflecting reduced local electron density caused by fluorine’s strong electron-withdrawing effect. As shown in Figure 3A, the progressive incorporation of DFBP is evidenced by the emergence and systematic increase in intensity of the C–F stretching bands highlighted in yellow. This trend confirms the successful modulation of fluorine content across the copolymer series and is consistent with the targeted increase in DFBP incorporation.  Thermal stability was evaluated by thermogravimetric analysis (TGA) before gas-permeation measurements to establish the materials’ suitability for relevant separation conditions. As shown in Figure 3B, all copolymers exhibit excellent thermal stability, with 5% weight-loss degradation temperatures (Td,5%) exceeding above 500 oC.

Figure 2.  (A) Representative19F NM Spectra of PIM-Fx copolymers and (B) 1H NMR Spectra of PIM-1 and PIM-Fx copolymers

Figure 3. (A) FTIR confirms PIM-Fx copolymers exhibiting systematically varied degrees of fluorination as reflected in the appearance of C-F bands highlighted in yellow shades. (B) TGA analysis demonstrating thermal stability of pure PIM-1 and PIM-Fx copolymers PIM-F(0.1)

3.2. Preparation and Characterization of PIM-Fx Thin Films

To isolate the effect of fluorination degree on gas-transport properties, a series of PIM-Fx films with systematically varied fluorine contents (10, 25, 50, 75, and 100 mol%) was prepared by solution casting. High-molecular-weight PIM-Fx powders were dissolved in chloroform at 3 wt%/v and cast onto leveled glass substrates. Following solvent evaporation under ambient conditions, the resulting films were immersed in methanol for three days and subsequently dried under vacuum at 100 °C for 1 h, as illustrated in Figure S1. Film thickness was controlled at approximately 100 μm across the series to minimize thickness-dependent effects and ensure consistency in permeation measurements; individual thickness values are provided in Table S1. Differential scanning calorimetry did not reveal a detectable glass-transition temperature for any PIM-Fx film below the onset of thermal degradation, consistent with the behavior of PIM-1.

To gain insight into the chain packing, the fresh PIM-Fx films were analyzed using wide angle x-ray scattering (WAXS) to estimate the interchain spacing to correlate with their membrane properties and gas separation properties.  Aside from that, FFV analysis was done from density measurements

3.3. Gas Permeation Properties of Fresh PIM-1 and PIM-Fx Films

Pure-gas permeation tests were conducted on the freshly cast films across all compositional ranges for the two condensable fluorinated gases (i.e., R-32 and R-125) at several pressure levels (30, 50, 80, and 100 psi) and at 35 °C. Gas permeability data and calculated ideal selectivity data for all fresh films are presented in Figure 5.   The R-32 and R125 permeability results through PIM-1 and the PIM-Fx copolymers reveal important correlations and insights. As shown, the incorporation of fluorinated moieties in the PIM-Fx copolymers results in significantly increased R-32 permeability compared to non-fluorinated PIM-1 across the testing pressure range. In particular, PIM-F0.1 with only 10 mol% fluorination degree exhibited a highest R-32 permeability of 5342 Barrer at 100 psi. This is especially important because R-32 is one of the most valuable third-generation F-gases, being one of the few HFCs that can be recycled and incorporated into new low- to moderate-GWP refrigerant blends. R-125 exhibited a much lower permeability than R-32 due to its larger kinetic diameter. These kinetic diameter-dependent permeability differences confirm diffusion-controlled transport through PIM-Fx copolymer films, favoring permeation of the smaller one-carbon R32 molecule over larger two-carbon R125 molecule. Additionally, all PIM-Fx copolymers displayed much improved R-32/R-125 ideal selectivity than pure PIM-1, signifying the contribution of sorption selectivity based on solution-diffusion mechanisms in these fluorinated ladder polymers. Specifically, an unprecedentedly high R-32/R-125 ideal selectivity of 1179 was achieved by PIM-F0.1 at 30 psi feed pressure. Due to their initial high selectivity at low pressure (e.g., 30 psi), the PIM-Fx copolymers retained excellent selectivity even at the highest testing pressure of 100 psi. For example, PIM-F0.5 exhibited a high R-32/R-125 ideal selectivity of 51 at 100 psi, while pure PIM-1’s selectivity dropped to be a little below 20 at the same feed pressure. K2CO3

AUTHOR INFORMATION

Corresponding Author

Ruilan Guo − Department of Chemical and Biomolecular Engineering, University of Notre Dame, Notre Dame, Indiana 46556, United States.

Email: rguo@nd.edu

Author

Benjamin Kamji− Department of Chemical and Biomolecular Engineering, University of Notre Dame, Notre Dame, Indiana 46556, United States.

Author Contributions:

B.K.: methodology, validation, formal analysis, investigation, data curation, writing − original draft.

R.G.: Conceptualization, resources, writing review and editing, supervision, project administration, funding acquisition.

Notes

The authors declare no competing financial interest

ACKNOWLEDGEMENTS

The authors acknowledge the financial support from the National Science Foundation (NSF) under award NSF-2330175. The authors thank the Center for Environmental Science and Technology (CEST) of the University of Notre Dame for the use of characterization facilities.

REFERENCES

(1)	Harders, A. N.; Uhl, H.; Xu, I.; Dixon, S.; Baca, K. R.; May, T.; Lundin, M. D.; Shiflett, M. B. Ionic Liquid Fluoropolymer Membranes for the Separation of R-410A: Understanding the Effect of Ionic Liquid on Membrane Characteristics and Separation Performance. J. Memb. Sci. 2024, 709. https://doi.org/10.1016/j.memsci.2024.123068.

(2)	Pardo, F.; Gutiérrez-Hernández, S. V.; Rodríguez-San Miguel, P.; Zarca, G.; Urtiaga, A. Polymer/Ionic Liquid Pilot Scale Membrane Prototype for the Recovery of Difluoromethane (R-32) from Refrigerant Mixtures. Sep. Purif. Technol. 2023, 320. https://doi.org/10.1016/j.seppur.2023.124115.

(3)	Harders, A. N.; Wallisch, L.; Lundin, M. D.; Le, C.; Zaher, G.; Atchison, E.; White, W.; Shiflett, M. B. Separation and Recycling of Hydrofluorocarbon Refrigerant Mixtures with Fluoropolymer-Coated Hollow Fiber Membranes; 2025; Vol. 11. https://www.science.org.

(4)	- International Energy Agency, I. The Future of Cooling Opportunities for Energy-Efficient Air Conditioning Together Secure Sustainable. www.iea.org/t&c/.

(5)	Laine, H. S.; Salpakari, J.; Looney, E. E.; Savin, H.; Peters, I. M.; Buonassisi, T. Meeting Global Cooling Demand with Photovoltaics during the 21st Century. Energy Environ. Sci. 2019, 12 (9), 2706–2716. https://doi.org/10.1039/c9ee00002j.

(6)	Jovell, D.; Pou, J. O.; Llovell, F.; Gonzalez-Olmos, R. Life Cycle Assessment of the Separation and Recycling of Fluorinated Gases Using Ionic Liquids in a Circular Economy Framework. ACS Sustain. Chem. Eng. 2022, 10 (1), 71–80. https://doi.org/10.1021/acssuschemeng.1c04723.

(7)	Harders, A. N.; Dixon, S.; Hines, B.; Lundin, M.; White, W.; Shiflett, M. B. Separation of Refrigerant Gases Using a Copolymer of Perfluoro(2,2-Dimethyl-1,3-Dioxole) (PDD) and Vinyl Acetate (VA). Ind. Eng. Chem. Res. 2023, 62 (37), 15148–15156. https://doi.org/10.1021/acs.iecr.3c01822.

(8)	Harders, A. N.; Wallisch, L.; Lundin, M. D.; Le, C.; Zaher, G.; Atchison, E.; White, W.; Shiflett, M. B. Separation and Recycling of Hydrofluorocarbon Refrigerant Mixtures with Fluoropolymer-Coated Hollow Fiber Membranes; 2025; Vol. 11. https://www.science.org.

(9)	Harders, A. N.; Sturd, E. R.; Vallier, J. E.; Corbin, D. R.; White, W. R.; Junk, C. P.; Shiflett, M. B. Selective Separation of HFC-32 from R-410A Using Poly(Dimethylsiloxane) and a Copolymer of Perfluoro(Butenyl Vinyl Ether) and Perfluoro(2,2-Dimethyl-1,3-Dioxole). J. Memb. Sci. 2022, 652. https://doi.org/10.1016/j.memsci.2022.120467.

(10)	García, E. J.; Bahamon, D.; Vega, L. F. Systematic Search of Suitable Metal-Organic Frameworks for Thermal Energy-Storage Applications with Low Global Warming Potential Refrigerants. ACS Sustain. Chem. Eng. 2021, 9 (8), 3157–3171. https://doi.org/10.1021/acssuschemeng.0c07797.

(11)	Jovell, D.; Pou, J. O.; Llovell, F.; Gonzalez-Olmos, R. Life Cycle Assessment of the Separation and Recycling of Fluorinated Gases Using Ionic Liquids in a Circular Economy Framework. ACS Sustain. Chem. Eng. 2022, 10 (1), 71–80. https://doi.org/10.1021/acssuschemeng.1c04723.

(12)	Tkachenko, I. M.; Belov, N. A.; Kobzar, Y. L.; Dorokhin, A. V.; Shekera, O. V.; Shantarovich, V. P.; Bekeshev, V. G.; Shevchenko, V. V. Synthesis of Fluorinated Poly(Arylene Ether)s with Dibenzodioxin and Spirobisindane Units from New Bis(Pentafluorophenyl)- and Bis(Nonafluorobiphenyl)-Containing Monomers. J. Fluor. Chem. 2017, 195, 1–12. https://doi.org/10.1016/j.jfluchem.2017.01.008.

(13)	Gutiérrez-Hernández, S. V.; Pardo, F.; Foster, A. B.; Gorgojo, P.; Budd, P. M.; Zarca, G.; Urtiaga, A. Outstanding Performance of PIM-1 Membranes towards the Separation of Fluorinated Refrigerant Gases. J. Memb. Sci. 2023, 675. https://doi.org/10.1016/j.memsci.2023.121532.

(14)	Pardo, F.; Gutiérrez-Hernández, S. V.; Rodríguez-San Miguel, P.; Zarca, G.; Urtiaga, A. Polymer/Ionic Liquid Pilot Scale Membrane Prototype for the Recovery of Difluoromethane (R-32) from Refrigerant Mixtures. Sep. Purif. Technol. 2023, 320. https://doi.org/10.1016/j.seppur.2023.124115.

(15)	Pardo, F.; Zarca, G.; Urtiaga, A. Effect of Feed Pressure and Long-Term Separation Performance of Pebax-Ionic Liquid Membranes for the Recovery of Difluoromethane (R32) from Refrigerant Mixture R410A. J. Memb. Sci. 2021, 618. https://doi.org/10.1016/j.memsci.2020.118744.

(16)	Harders, A. N.; Uhl, H.; Xu, I.; Dixon, S.; Baca, K. R.; May, T.; Lundin, M. D.; Shiflett, M. B. Ionic Liquid Fluoropolymer Membranes for the Separation of R-410A: Understanding the Effect of Ionic Liquid on Membrane Characteristics and Separation Performance. J. Memb. Sci. 2024, 709. https://doi.org/10.1016/j.memsci.2024.123068.

(17)	Snap, E. TRANSITIONING TO LOW-GWP ALTERNATIVES in Domestic Refrigeration Background. http://www.ecomatesystems.com/.

(18)	Pardo, F.; Zarca, G.; Urtiaga, A. Effect of Feed Pressure and Long-Term Separation Performance of Pebax-Ionic Liquid Membranes for the Recovery of Difluoromethane (R32) from Refrigerant Mixture R410A. J. Memb. Sci. 2021, 618. https://doi.org/10.1016/j.memsci.2020.118744.

(19)	Shiflett. (12) United States Patent Field of Classification Search; 2014; Vol. 52.

(20)	Shiflett, M.; Yokozeki, A. Separation of Difluoromethane and Pentafluoroethane by Extractive Distillation Using Ionic Liquid. Chim. Oggi 2006, 24.

(21)	Harders, A. N.; Dixon, S.; Hines, B.; Lundin, M.; White, W.; Shiflett, M. B. Separation of Refrigerant Gases Using a Copolymer of Perfluoro(2,2-Dimethyl-1,3-Dioxole) (PDD) and Vinyl Acetate (VA). Ind. Eng. Chem. Res. 2023, 62 (37), 15148–15156. https://doi.org/10.1021/acs.iecr.3c01822.

(22)	Baca, K. R.; Al-Barghouti, K.; Wang, N.; Bennett, M. G.; Matamoros Valenciano, L.; May, T. L.; Xu, I. V.; Cordry, M.; Haggard, D. M.; Haas, A. G.; Heimann, A.; Harders, A. N.; Uhl, H. G.; Melfi, D. T.; Yancey, A. D.; Kore, R.; Maginn, E. J.; Scurto, A. M.; Shiflett, M. B. Ionic Liquids for the Separation of Fluorocarbon Refrigerant Mixtures. Chemical Reviews. American Chemical Society May 8, 2024, pp 5167–5226. https://doi.org/10.1021/acs.chemrev.3c00276.

(23)	Snap, E. TRANSITIONING TO LOW-GWP ALTERNATIVES in Domestic Refrigeration Background. http://www.ecomatesystems.com/.

(24)	SATILMIŞ, B. Adsorption of Aniline from Aqueous System by Highly Fluorinated Polymers of Intrinsic Microporosity (PIM-2). Iğdır Üniversitesi Fen Bilimleri Enstitüsü Dergisi 2020, 10 (3), 1886–1898. https://doi.org/10.21597/jist.725624.

(25)	Emamverdi, F.; Huang, J.; Razavi, N. M.; Bojdys, M. J.; Foster, A. B.; Budd, P. M.; Böhning, M.; Schönhals, A. Molecular Mobility and Gas Transport Properties of Mixed Matrix Membranes Based on PIM-1 and a Phosphinine Containing Covalent Organic Framework. Macromolecules 2024, 57 (4), 1829–1845. https://doi.org/10.1021/acs.macromol.3c02419.

(26)	Shiflett, M. B.; Yokozeki, A. Binary Vapor-Liquid and Vapor-Liquid-Liquid Equilibria of Hydrofluorocarbons (HFC-125 and HFC-143a) and Hydrofluoroethers (HFE-125 and HFE-143a) with Ionic Liquid [Emim][Tf2N]. J. Chem. Eng. Data 2008, 53 (2), 492–497. https://doi.org/10.1021/je700588d.

(27)	Asensio-Delgado, S.; Pardo, F.; Zarca, G.; Urtiaga, A. Absorption Separation of Fluorinated Refrigerant Gases with Ionic Liquids: Equilibrium, Mass Transport, and Process Design. Separation and Purification Technology. Elsevier B.V. December 1, 2021. https://doi.org/10.1016/j.seppur.2021.119363.

(28)	Asensio-Delgado, S.; Jovell, D.; Zarca, G.; Urtiaga, A.; Llovell, F. Thermodynamic and Process Modeling of the Recovery of R410A Compounds with Ionic Liquids. International Journal of Refrigeration 2020, 118, 365–375. https://doi.org/10.1016/j.ijrefrig.2020.04.013.

(29)	Wanigarathna, D. K. J. A.; Gao, J.; Takanami, T.; Zhang, Q.; Liu, B. Adsorption Separation of R-22, R-32 and R-125 Fluorocarbons Using 4A Molecular Sieve Zeolite. ChemistrySelect 2016, 1 (13), 3718–3722. https://doi.org/10.1002/slct.201600689.

(30)	Vopicka, O.; De Angelis, M. G.; Sarti, G. C.; Yampolskii, Y.; Finkelshtein, E.; Bermeshev, M. Sorption and Diffusion of Gases and Vapors in Poly (Exo,Endo-3,4- Bis(Trimethylsilyl)Tricyclononene). In Procedia Engineering; Elsevier Ltd, 2012; Vol. 44, pp 760–761. https://doi.org/10.1016/j.proeng.2012.08.560.

(31)	Pinnau, I.; Toy, L. G. Transport of Organic Vapors through Poly( 1-Trimethylsilyl-1-Propyne); 1996; Vol. 116.

(32)	Budd, P. M.; Ghanem, B. S.; Makhseed, S.; McKeown, N. B.; Msayib, K. J.; Tattershall, C. E. Polymers of Intrinsic Microporosity (PIMs): Robust, Solution-Processable, Organic Nanoporous Materials. Chemical Communications 2004, 4 (2), 230–231. https://doi.org/10.1039/b311764b.

(33)	Abedini, R.; Nezhadmoghadam, A. APPLICATION OF MEMBRANE IN GAS SEPARATION PROCESSES: ITS SUITABILITY AND MECHANISMS.

(34)	Gutiérrez-Hernández, S. V.; Pardo, F.; Foster, A. B.; Gorgojo, P.; Budd, P. M.; Zarca, G.; Urtiaga, A. Outstanding Performance of PIM-1 Membranes towards the Separation of Fluorinated Refrigerant Gases. J. Memb. Sci. 2023, 675. https://doi.org/10.1016/j.memsci.2023.121532.

(35)	Ghasemi Estahbanati, E.; Omidkhah, M.; Ebadi Amooghin, A. Preparation and Characterization of Novel Ionic Liquid/Pebax Membranes for Efficient CO2/Light Gases Separation. Journal of Industrial and Engineering Chemistry 2017, 51, 77–89. https://doi.org/10.1016/j.jiec.2017.02.017.

(36)	Pardo, F.; Gutiérrez-Hernández, S. V.; Rodríguez-San Miguel, P.; Zarca, G.; Urtiaga, A. Polymer/Ionic Liquid Pilot Scale Membrane Prototype for the Recovery of Difluoromethane (R-32) from Refrigerant Mixtures. Sep. Purif. Technol. 2023, 320. https://doi.org/10.1016/j.seppur.2023.124115.

(37)	Pardo, F.; Zarca, G.; Urtiaga, A. Effect of Feed Pressure and Long-Term Separation Performance of Pebax-Ionic Liquid Membranes for the Recovery of Difluoromethane (R32) from Refrigerant Mixture R410A. J. Memb. Sci. 2021, 618. https://doi.org/10.1016/j.memsci.2020.118744.

(38)	Li, M.; Zhang, X.; Zeng, S.; Bai, L.; Gao, H.; Deng, J.; Yang, Q.; Zhang, S. Pebax-Based Composite Membranes with High Gas Transport Properties Enhanced by Ionic Liquids for CO2 Separation. RSC Adv. 2017, 7 (11), 6422–6431. https://doi.org/10.1039/c6ra27221e.

(39)	Pardo, F.; Zarca, G.; Urtiaga, A. Separation of Refrigerant Gas Mixtures Containing R32, R134a, and R1234yf through Poly(Ether- Block-Amide) Membranes. ACS Sustain. Chem. Eng. 2020, 8 (6), 2548–2556. https://doi.org/10.1021/acssuschemeng.9b07195.

(40)	Jue, M. L.; Lively, R. P. Targeted Gas Separations through Polymer Membrane Functionalization. Reactive and Functional Polymers. Elsevier B.V. 2015, pp 88–110. https://doi.org/10.1016/j.reactfunctpolym.2014.09.002.

(41)	Pardo, F.; Gutiérrez-Hernández, S. V.; Zarca, G.; Urtiaga, A. Toward the Recycling of Low-GWP Hydrofluorocarbon/Hydrofluoroolefin Refrigerant Mixtures Using Composite Ionic Liquid-Polymer Membranes. ACS Sustain. Chem. Eng. 2021, 9 (20), 7012–7021. https://doi.org/10.1021/acssuschemeng.1c00668.

(42)	Merkel, T. C.; Bondar, V. I.; Nagai, K.; Freeman, B. D.; Pinnau, I. Gas Sorption, Diffusion, and Permeation in Poly(Dimethylsiloxane). J. Polym. Sci. B Polym. Phys. 2000, 38 (3), 415–434. https://doi.org/10.1002/(SICI)1099-0488(20000201)38:3<415::AID-POLB8>3.0.CO;2-Z.

(43)	Ruan, X.; Dai, Y.; Du, L.; Yan, X.; He, G.; Li, B. Further Separation of HFC-23 and HCFC-22 by Coupling Multi-Stage PDMS Membrane Unit to Cryogenic Distillation. Sep. Purif. Technol. 2015, 156, 673–682. https://doi.org/10.1016/j.seppur.2015.10.064.

(44)	Yu, M.; Foster, A. B.; Kentish, S. E.; Scholes, C. A.; Budd, P. M. Recent Progress in Thin Film Composite Membranes Based on the Polymer of Intrinsic Microporosity PIM-1: Preparation, Properties and Performance. Journal of Membrane Science. Elsevier B.V. April 1, 2025. https://doi.org/10.1016/j.memsci.2025.123844.

(45)	McKeown, N. B.; Budd, P. M. Exploitation of Intrinsic Microporosity in Polymer-Based Materials. Macromolecules 2010, 43 (12), 5163–5176. https://doi.org/10.1021/ma1006396.

(46)	Fuoco, A.; Satilmis, B.; Uyar, T.; Monteleone, M.; Esposito, E.; Muzzi, C.; Tocci, E.; Longo, M.; De Santo, M. P.; Lanč, M.; Friess, K.; Vopička, O.; Izák, P.; Jansen, J. C. Comparison of Pure and Mixed Gas Permeation of the Highly Fluorinated Polymer of Intrinsic Microporosity PIM-2 under Dry and Humid Conditions: Experiment and Modelling. J. Memb. Sci. 2020, 594. https://doi.org/10.1016/j.memsci.2019.117460.